## Slide 1
Origin of the band gap for ionic materials : a data driven approach
The band gap (Eg) is one of the crucial parameters in the determination of the thermoelectric (TE) performance of a semiconducting material. Herein, we present a data driven investigation of the origin of the band gap and its linkage to elemental properties, mainly electronegativity. By leveraging upon the abundance of data available in the Materials Project (MP) database, we found 10 new chalcogenide based compounds with narrow band gap and possibly low thermal conductivity. These compounds could be very suitable for near room temperature (RT) cooling applications.
Abstract
Author: Jose Recatala Gomez

## Slide 2: Motivation
TE Performance
Efficiency (η)
zT
S2σ
κ -1
Eg
1. He et. al. Science 357, 1369 (2007)
2. H. J. Goldsmid et. al., J. Electron. Mater. 28, 869–872 (1999)
3. Gibbs, Zachary M., et.al, Applied Physics Letters 106, 2 (2015)
Valid for degenerate semiconductors in bipolar regime
The Eg will determine Smax, which in turn will determine zTmax
The performance of TE materials is low in comparison with other technologies. A better performance can only be achieved by the synergistic enhancement of the components of the dimensionless figure-of-merit zT = S2σT/κ

## Slide 3
Band gap: main origin
U = 0
U ≠ 0
4. C Kittle, Introduction to Solid State Physics
5. Dimitrov et. al. Journal of Solid State Chemistry 196 (2012) 574–578
dx
For ionic solids, the band gap (crystal potential, U) is directly proportional to the polarizability (α) and inversely proportional to the ionisation energy (IE)
α
Clausius-Mossotti relation

## Slide 4
0
E
) *
EA
IE
EC
EV
EF
6. Zeier, W.G et. al. Angewandte Chemie International Edition, 55(24), pp.6826-6841
We can use IE as metric, but we can also use EN (which will give additional information regarding the bonding)
Band gap: correlation with electronegativity
α
*EN in Pauling scale
Direct correlation between Eg and EN is expected
Electronegativity (EN): the power of an atom in a molecule to attract electrons to itself
Ionisation Energy (IE): energy required to remove an electron from a neutral atom in its gaseous phase
6. Pauling, L., J. Chem. Educ., 1992, 69 (7), p 519

## Slide 5: Problem Statement
Can we, through a data-driven approach, find materials that have low EN to find narrow Eg materials for near room temperature TE?

## Slide 6
Methodology
Focused on ABX2 chalcogenides
Historically, good TE materials
Form a large subset of available data on materialsproject.org
58 S based chalcogenides
41 Se based chalcogenides
23 Te based chalcogenides
Dataset
Materials Project is an open database whose goal is the democratisation of knowledge by compiling diverse theoretical data (elasticity, band structures and band gaps …)
Data mining with Matminer
7.A. Jain et. al. APL Materials, 2013, 1(1), 011002.
Due to inaccuracies intrinsic to the dataset, a strict screening criteria is set
Screening criteria:
0.16 ≥ Eg ≤ 4 eV
Ehull = 0
Must contain a chalcogenide (S, Se, Te)
High symmetry compounds: ≥ 4 symmetry operations
8. Ward, L et. al. Comput. Mater. Sci. 152, 60-69 (2018).
Guin et. al Energy Environ. Sci., 2013,6, 2603-2608

## Slide 7
We define a new, more meaningful way to express the electronegativity in ABX2 ternary chalcogenides, the average range EN:
AgBiSe2
AgBiS2
TlInS2
ScTlSe2
KGdTe2
NaCrSe2
TlBiTe2
CrAuS2
TlBiSe2
GdTlTe2
This metric is an indicator of the nature of bonding in the materials
Limit of low Avg range EN  Covalent bonding
Limit of high Avg range EN  Ionic bonding
Results: ABX2 compounds with trigonal structure and space group of 166
From: 9.Snyder, G. J. et. al. Nat. Mater. 7, 105–114 (2008).
Compounds with Eg < 1 eV will show Smax near room temperature
Expected trend (Clausius-Mossotti)

## Slide 8
Conclusions
The lower the electronegativity difference, the narrower the band gap and the more covalent the bonding
Successful data-driven discovery in the family of ABX2 (X = S, Se, Te), where preliminary results for a few compounds are available, but other materials within this family remain unexplored
Our study recommends 10 unexplored compounds as potential candidates for near room temperature thermoelectric applications
Analysis and hypothesis